NEW ENGINEERING MATERIALS DEVELOPMENT FOR A SELF-RELIANT NIGERIAN ECONOMY

Ihom, A.P.

Department of Mechanical and Aerospace Engineering, Faculty of Engineering, University of Uyo, Akwa Ibom State-Nigeria.

Author’s Corresponding Address: 08035813571; ihomaondona@uniuyo.edu.ng

Paper Presented at the 6th International Conference on Research and Innovations in Engineering Organized by the Faculty of Engineering, University of Uyo with the theme: Engineering Solutions for a Self-Reliant Nigerian Economy, held at the 250 Capacity Engineering Lecture Hall at the Main Campus on the 8-9th October, 2026.

INTRODUCTION

The 21st Century has witnessed unprecedented innovations and development of new materials which have never before been matched in history. Structural wood has been improved upon to be 10 times stronger than steel and 6 times lighter, by the Chinese and Americans. The Chinese have developed advanced structural ceramics which has very high refractoriness and ductility that can be used for rockets and missile and space applications. The list is endless covering all classes of materials. Engineering materials are fundamental to technological development because virtually every engineered system depends on materials with appropriate mechanical, thermal, electrical, chemical, and environmental characteristics. Conventional engineering materials such as steels, aluminium alloys, titanium alloys, ceramics, polymers, concrete, and fibre-reinforced composites have enabled major developments in transportation, infrastructure, manufacturing, energy generation, and aerospace technology. Nevertheless, the increasing complexity of modern engineering systems has exposed important limitations in the performance envelope of conventional materials (Ihom & Offiong, 2018; Eswarappa, et al., 2023; Han, et al., 2024; Hsu, et al., 2024; Sandra, 2025).

Contemporary aerospace systems, for example, require materials that can tolerate high temperature, oxidation, mechanical loading, thermal shock, and radiation. Similarly, the rapid development of drones and robotic war vehicle machines, electric vehicles and renewable-energy systems requires materials that combine low density, high mechanical performance, electrochemical stability, electrical conductivity, and long service life. Electronic and biomedical technologies impose additional requirements such as flexibility, miniaturization, biocompatibility, high surface area, and multifunctionality. These increasingly demanding requirements have stimulated the development of materials whose properties can be deliberately controlled across multiple length scales (Han et al., 2024).

The concept of a “new engineering material” consequently extends beyond the discovery of a new chemical composition. Modern materials engineering increasingly involves the simultaneous control of composition, atomic arrangement, microstructure, interfaces, nanoscale features, and macroscopic architecture. This development has produced several important material families, including high-entropy materials (HEMs), two-dimensional materials, MXenes, ultra-high-temperature ceramics (UHTCs), metamaterials, aerogels, self-healing materials, advanced nanocomposites, and sustainable bio-derived materials (Ogbodo, et al., 2015; Ihom, et al., 2023; Wyatt, et al., 2024) .

High-entropy materials are particularly significant because the high-entropy concept has expanded from metallic alloys into ceramics, polymers, composites, and low-dimensional materials. Their large compositional space provides opportunities to develop multifunctional materials with combinations of mechanical, magnetic, electronic, electrochemical, catalytic, thermal, and hydrogen-related properties (Han et al., 2024).

The development of high-entropy materials has also challenged traditional approaches to materials design. Conventional alloy development frequently begins with a dominant element and introduces smaller concentrations of alloying elements. In contrast, high-entropy design permits several principal elements to occupy a material's crystal structure. This approach introduces complex chemical environments and potentially useful local atomic configurations (Jain, 2009; Sun & Dai, 2024).

Two-dimensional materials constitute another major area of development. Since the emergence of graphene and related materials, researchers have explored numerous atomically thin materials with unique electronic, mechanical, optical, thermal, and chemical properties. Among these, MXenes have attracted particular attention because their high electrical conductivity, layered structure, surface functionality, and chemical tunability make them relevant to energy storage, sensors, electromagnetic shielding, catalysis, and environmental technologies (Schweidler, et al., 2024).

At the high-temperature end of materials engineering, ultra-high-temperature ceramics have emerged as critical materials for extreme environments. UHTCs based on transition-metal carbides, nitrides, and borides can exhibit melting temperatures above 4,000 °C, high thermal conductivity, and exceptional stiffness, making them attractive for hypersonic vehicles, atmospheric-entry systems, rocket propulsion, and other extreme-temperature technologies (Wyatt et al., 2024).

Another important change is the growing recognition that material architecture can be engineered independently of chemical composition. Metamaterials and architected materials exploit carefully designed geometries to obtain unusual mechanical, acoustic, thermal, electromagnetic, or optical responses. Additive manufacturing has accelerated this development because complex three-dimensional architectures that would be difficult to manufacture using conventional techniques can now be fabricated with increasing precision.

At the same time, sustainability has become a central consideration in materials research. The environmental consequences associated with extraction of raw materials, energy-intensive processing, manufacturing waste, and end-of-life disposal have created pressure to develop materials based on renewable resources, recycled materials, low-carbon processes, and circular manufacturing principles (Ihom & Offiong, 2018; Eswarappa, et al., 2023; Han, et al., 2024; Hsu, et al., 2024; Sandra, 2025). .

Consequently, modern engineering-materials research is increasingly characterized by convergence. High-entropy concepts are being combined with ceramics and two-dimensional materials; additive manufacturing is being combined with high-entropy alloys and metamaterials; nanomaterials are being integrated into polymers and aerogels; and artificial intelligence is being used to accelerate the identification of promising compositions and processing conditions (Hsu, et al., 2024).

Nigeria has come of age to become a country with a self-reliant economy, unfortunately instead of progressing economically Nigeria seems to be retrogressing economically and technologically this abnormality can be tied to the absence of the development of new engineering materials, which comes under value addition. A country cannot be selling her natural resources in raw form and expects to be self-reliant. This explains why Nigeria has remained an economically dependent country. A self-reliant economy is an economic system in which a country develops enough productive capacity, skills, institutions, technology, and resources to meet a substantial share of its own essential needs rather than depending excessively on imports, foreign aid, or external financing (OECD, 2023; NBS, 2023; CBN, 2023; ADB 2024; Ihom & Odeh, 2025).

Self-reliance does not mean complete economic isolation. A self-reliant country can still trade internationally, attract investment, and participate in global markets. The central idea is to develop strong domestic productive capacity so that international trade complements the economy rather than becoming a source of excessive vulnerability. On the other hand completely self-sufficient economy attempts to produce virtually everything domestically; this is the least status Nigeria should maintain, unfortunately it is also not here (UN, 2020; WB, 2022; WTO, 2023; WB, 2024).

The objective of this review is to examine major emerging classes of engineering materials; and how these new engineering materials which are as a result of value addition can lead to a self-reliant Nigerian economy.

2.0 SELF-RELIANT ECONOMY EXPLAINED

Economic self-reliance refers to the capacity of a country to utilize its domestic resources, institutions, skills, technologies, and productive capabilities to satisfy important economic needs and withstand external disruptions. It emphasizes internal capacity building while recognizing that international trade and cooperation remain important components of economic development (Rodrik, 2004).

A self-reliant economy is therefore characterized by the capacity to produce essential goods and services, process domestic raw materials, develop human and technological capabilities, mobilize domestic financial resources, and maintain productive relationships with international markets. The concept can be understood through three major dimensions.

### Productive Self-Reliance

Productive self-reliance concerns a country's ability to produce goods and services domestically. It includes agriculture, manufacturing, construction, energy, transportation, digital services, and other productive sectors. For Nigeria, productive self-reliance would involve increasing domestic production of food, manufactured products, machinery, construction materials, pharmaceuticals, textiles, and other strategically important products (Rodrik, 2004; NBS, 2023; CBN, 2023; ADB, 2024).

### 2.2 Technological Self-Reliance

Technological self-reliance refers to the ability to acquire, adapt, maintain, improve, and develop technologies appropriate to domestic needs. It does not necessarily require a country to invent every technology it uses.

A technologically self-reliant economy should possess sufficient domestic technical expertise to understand imported technologies, maintain equipment, adapt technologies to local conditions, and progressively develop indigenous innovations. This where Nigeria needs to be in order to be technological self-reliant.

### Financial and Institutional Self-Reliance

Financial self-reliance involves the ability to mobilize domestic savings and investment resources to finance economic development. Institutional self-reliance involves the existence of effective institutions capable of implementing policies, regulating markets, enforcing contracts, collecting revenue, and supporting productive activities. Together, these dimensions provide the foundation for sustainable economic independence. Once Nigeria attains financial and institutional self-reliance our foreign debts will reduce and disappear with time. This explains the essence of this paper (OECD, 2023; WB, 2024).

## 3. Benefits of a Self-Reliant Economy

### 3.1 Employment Creation

Expanding domestic agriculture, manufacturing, processing, construction, technology, and services can generate employment opportunities. Domestic production creates both direct and indirect employment. For example, the development of a food-processing industry can create jobs not only in factories but also in farming, transportation, packaging, maintenance, logistics, marketing, and retail.

### 3.2 Improved Food Security

Greater agricultural productivity and domestic food processing can reduce vulnerability to disruptions in international food markets. It can also improve the availability and affordability of food when supported by appropriate infrastructure, storage, transportation, and market systems.

### 3.3 Reduction of Import Dependence

A productive domestic economy can reduce dependence on imported goods where local production is economically viable. Reducing unnecessary import dependence can also reduce pressure on foreign-exchange resources. However, imports of machinery, technology, intermediate inputs, and specialized products may remain necessary and can contribute to domestic productivity.

### 3.4 Foreign-Exchange Stability

### An economy that exports a diversified range of goods and services while reducing excessive dependence on imported consumer products can improve its external position. For Nigeria, increased exports of processed agricultural products, manufactured goods, minerals, petrochemicals, digital services, and other products could broaden sources of foreign exchange.

### 3.5 Industrial Development

Economic self-reliance encourages the establishment of domestic industries capable of processing raw materials and producing intermediate and final goods. Industrialization can increase productivity, facilitate technological learning, create skilled employment, and expand the tax base.

### 3.6 Technological Development

Domestic production creates opportunities for learning by doing. Engineers, technicians, scientists, entrepreneurs, and workers acquire practical knowledge through production and innovation. Over time, this can contribute to the development of indigenous technological capabilities.

### 3.7 Greater Economic Resilience

An economy with diversified production and stronger domestic supply chains can be better positioned to respond to external disruptions. The COVID-19 pandemic demonstrated the vulnerabilities associated with highly interconnected supply chains and dependence on external sources for certain essential products (United Nations Conference on Trade and Development [UNCTAD], 2020).

### 3.8 Poverty Reduction and Inclusive Development

Self-reliance can contribute to poverty reduction when increased production translates into productive employment, higher incomes, improved infrastructure, and broader access to economic opportunities. The benefits, however, depend on the inclusiveness of economic policies and the distribution of opportunities (UNCTAD, 2020; WTO, 2023; WB, 2024).

### 3.8.1 Self-Reliance Versus Economic Self-Sufficiency

The two concepts are related but different as indicated in Table 1.

Table 1 Difference between Self-Reliance and Economic Self-Sufficiency

| Self-reliant economy | Completely self-sufficient economy |
| --- | --- |
| Produces many essential goods and services domestically | Attempts to produce virtually everything domestically |
| Participates actively in international trade | Minimizes dependence on international trade |
| Imports goods when economically useful or necessary | Attempts to minimize imports |
| Builds domestic productive and technological capacity | Emphasizes domestic production regardless of comparative advantage |
| Seeks resilience against external shocks | Seeks maximum economic independence |

Source: Rodrik, 2004; UNCTAD, 2020; World Bank, 2024

Thus, economic self-reliance is generally more practical than complete self-sufficiency in a highly interconnected global economy.

4. SELF-RELIANT ECONOMIES

Many countries of the world have self-reliant economies, these countries don’t import everything, their economies are not import-dependent and they don’t depend on foreign aid and borrowing rather they assist other countries. Countries like Japan and China are good examples of self-reliant economies. They import goods only when economically useful or necessary and they have built domestic productive and technological capacity. These two countries have good resilience against external shocks. Not everything that happens outside of their countries affect their economies. This explains why the United States of America was always complaining of trade deficit with these countries. The key features of a self-reliant economy are listed below:

a. Strong domestic production
The country produces a significant proportion of the food, manufactured goods, energy, and services required by its population.

b. Agricultural productivity and food security
Farmers have access to land, finance, improved seeds, machinery, irrigation, storage, processing facilities, and markets. Agriculture therefore moves beyond subsistence production toward commercial and industrial production.

c. Industrial development
Raw materials are processed domestically instead of being exported mainly in their unprocessed form. For example, crude agricultural or mineral resources can be converted into finished or semi-finished products within the country.

d. Human-capital development
A self-reliant economy requires engineers, scientists, technicians, entrepreneurs, teachers, healthcare professionals, skilled artisans, and other workers capable of solving domestic production and technological problems.

e. Technological capability
The country develops the ability to adapt, manufacture, maintain, and eventually innovate technologies relevant to its economy rather than relying entirely on imported technology.

f. Access to domestic finance
Local banks, development-finance institutions, capital markets, pension funds, and other financial institutions provide funding for productive investment.

g. Energy security
Reliable and reasonably affordable electricity and other forms of energy are essential because manufacturing, agriculture, transportation, mining, and digital services all depend on energy.

h. Diversified exports
Although self-reliance emphasizes domestic production, exports remain important. A diversified export base generates foreign exchange and reduces dependence on a small number of commodities.

### i. Efficient Utilization of Domestic Resources

A self-reliant economy begins with effective utilization of available resources. These include land, minerals, agricultural resources, energy, water, human skills, financial resources, and entrepreneurial capabilities. Nigeria possesses substantial natural resources, but the existence of resources alone does not guarantee economic development. Resources must be transformed through technology, investment, skills, infrastructure, and institutions into productive economic activities.

### j. Value Addition

Value addition is a fundamental principle of self-reliance. Countries that primarily export raw materials and import finished products may capture only a relatively small portion of the potential value associated with their resources. For example, instead of exporting agricultural commodities in raw form, domestic industries can process them into food products, textiles, oils, beverages, animal feeds, and other manufactured products. Similarly, mineral resources can be processed domestically to create intermediate and finished industrial products.

### k. Economic Diversification

A self-reliant economy should not depend excessively on one commodity, sector, market, or source of revenue. Diversification reduces vulnerability to sector-specific and external shocks. For Nigeria, diversification is particularly relevant because petroleum has historically played a major role in government revenue and foreign-exchange earnings. Developing agriculture, manufacturing, mining, construction, digital services, renewable energy, tourism, and other productive sectors can broaden the country's economic base.

### l. Human Capital Development

Human beings constitute a central productive resource in any economy. Self-reliance requires a workforce capable of operating modern industries, conducting research, managing enterprises, designing infrastructure, and solving technological problems. Investment in universities, polytechnics, technical colleges, vocational education, apprenticeships, and industry-based training is therefore essential.

### m. Technological Innovation

Technology contributes to productivity and competitiveness. A self-reliant economy must therefore encourage research, development, innovation, technology transfer, and entrepreneurship. The objective should be to move progressively from merely consuming imported technology toward adapting and developing technologies that address local economic and social needs.

### n. Domestic Entrepreneurship

Small, medium, and large domestic enterprises are important instruments of economic self-reliance. Domestic businesses create employment, develop supply chains, introduce innovations, and retain a larger share of economic value within the country. Policies should therefore encourage entrepreneurship while ensuring that businesses operate in a competitive and productive environment.

### o. Food and Energy Security

Food and energy are strategic sectors because disruptions in either can affect virtually every other part of the economy. A self-reliant economy should therefore increase agricultural productivity and develop reliable energy infrastructure. Food security does not require producing every food item domestically, just as energy security does not necessarily require reliance on a single energy source. The emphasis should be on resilience, affordability, diversification, and productive capacity.

### p. Strategic International Engagement

Self-reliance does not imply withdrawal from global markets. Rather, countries should engage internationally in ways that support domestic productive capacity. Foreign investment, international trade, technology transfer, development finance, and international partnerships can contribute to self-reliance when they strengthen domestic capabilities and productive activities (Rodrik, 2004; UNCTAD, 2020; WTO, 2023; CBN, 2023; WB, 2024; ADB, 2024).

5. CURRENT NIGERIAN ECONOMY

For Nigeria, economic self-reliance could involve moving from a predominantly resource-exporting and import-dependent structure toward greater domestic production and value addition. This is very important if Nigeria wants to be a self-reliant economy. The development of new engineering materials could serve as a spring board for achieving economic self-reliance since its part of value addition which bring more profit and technological know-how than resource trading or raw materials trading (NBS, 2023; CBN, 2023; WB, 2024; Ihom & Odeh, 2025). The current situation of the Nigerian Economy can be summarized as follows as shown in Table 2.

## Table 2: Overall Current Economic Picture of the Nigerian Economy.

| Indicator | Current position |
| --- | --- |
| Economic growth | Strengthening; 4.43% in Q2 2026 |
| Inflation | Much lower than earlier peaks, but cost-of-living pressure remains |
| Naira | More stable recently |
| Foreign reserves | Improving |
| Oil production | Increasing |
| Non-oil sector | Important source of growth |
| Government finances | Still under significant pressure |
| Public debt | Moderate relative to GDP, but debt-service costs are high |
| Poverty | Remains very high |
| Food security | Significant concern |
| Infrastructure | Major constraint |
| Economic diversification | Progressing but incomplete |
| Long-term outlook | Dependent on continued reforms, productivity growth and inclusive development |

### Source: IMF, World Bank, and Reuters, 2026

Nigeria's economy in 2026 can best be described as an economy undergoing significant structural adjustment and showing improved macroeconomic stability, but with substantial social and structural challenges still unresolved and exhibiting serious inflation as a result of its dependent nature on imported goods and the Dollar.

For example the illustrations below can pull Nigeria out of the current narrative of economically dependent country:

Agriculture → agro-processing → manufacturing → domestic and export markets

Instead of exporting agricultural commodities with limited processing, investment can support food processing, packaging, textile production, leather processing, bio-based materials, machinery, and other manufacturing activities (Ihom & Odeh, 2025).

Similarly:

Crude oil → refining → petrochemicals → plastics, fertilizers and other industrial products

The objective would be to capture more value domestically while developing the skills, infrastructure, businesses, and institutions needed to support these industries.

## 6. NIGERIA'S ECONOMIC STRUCTURE AND THE NEED FOR GREATER SELF-RELIANCE

Nigeria is one of Africa's largest economies and possesses considerable natural and human resources. The country has substantial agricultural potential, petroleum resources, solid minerals, a large domestic market, a growing technology sector, and significant entrepreneurial activity.

Despite these advantages, structural constraints have limited the transformation of resources into broad-based productive capacity. The World Bank (2022) emphasized that Nigeria's development challenges include weak productivity growth, inadequate infrastructure, fiscal pressures, and structural dependence on oil.

The petroleum sector has historically generated a substantial share of Nigeria's foreign-exchange earnings and public revenues. This dependence creates vulnerability when international oil prices decline or petroleum production is disrupted.

Agriculture represents another major area of potential. Nigeria has considerable arable land and a large agricultural workforce, but productivity, storage, irrigation, mechanization, transportation, processing, access to finance, and market infrastructure remain important constraints.

Manufacturing also faces challenges involving energy costs, infrastructure, financing, imported inputs, logistics, technology, and regulatory conditions.

Consequently, economic self-reliance in Nigeria should be approached as a process of structural transformation rather than simply an attempt to reduce imports (NBS, 2023; CBN, 2023; WB, 2024; Ihom & Odeh, 2025).

## 6.1 Major Challenges to Economic Self-Reliance in Nigeria

### 6.1.1 Inadequate Infrastructure

Infrastructure deficits remain one of the major constraints to domestic production. Unreliable electricity, inadequate transportation networks, inefficient logistics, and limitations in water infrastructure increase production costs. Industrial enterprises require dependable infrastructure to compete domestically and internationally.

### 6.1.2 Energy Constraints

Manufacturing and other productive sectors require reliable and affordable electricity. Where businesses must depend heavily on alternative energy sources, production costs can increase significantly .Improving electricity generation, transmission, distribution, and alternative energy systems is therefore essential.

### 6.1.3 Limited Access to Long-Term Finance

Many businesses, particularly small and medium-sized enterprises, face difficulties obtaining affordable long-term financing. High financing costs and limited access to patient capital can restrict investment in machinery, research, expansion, and technology.

### 6.1.4 Technology Dependence

Nigeria continues to rely substantially on imported machinery, industrial equipment, and technologies. Importing technology is not inherently problematic; the challenge arises when domestic capacity to operate, maintain, adapt, and improve imported technologies is limited.

### 6.1.5 Skills Gaps

The availability of appropriately trained workers is essential for industrial development. Gaps between educational curricula and labor-market requirements can limit productivity. Technical and vocational education therefore requires greater attention.

### 6.1.6 Policy Inconsistency

Investors require predictable policies to make long-term investment decisions. Frequent changes in taxation, trade regulations, foreign-exchange arrangements, and other economic policies can increase uncertainty. Long-term industrial development requires policy consistency and credible institutions.

### 6.1.7 Weak Research and Development Linkages

Nigeria possesses universities and research institutions, but the connection between research organizations and industry can be strengthened. Commercialization of research findings remains an important challenge.

### 6.1.8 Dependence on Raw Commodity Exports

The export of commodities with limited domestic processing can reduce opportunities for value addition and industrial development. Greater domestic processing can increase the economic value captured within Nigeria.

### 6.1.9 Institutional and Governance Constraints

Effective economic transformation requires institutions capable of implementing policies efficiently and transparently. Weak regulatory coordination, administrative delays, corruption risks, and inadequate enforcement can reduce investment and productivity.

### 6.1.10 Insecurity and Social Disruptions

Insecurity can affect agricultural production, transportation, investment, and industrial activities. A stable economic environment is essential for productive investment and long-term development (Rodrik, 2004; UNCTAD, 2020; WTO, 2023; CBN, 2023; WB, 2024; ADB, 2024; Reuters, 2026).

7. NEW ENGINEERING MATERIALS EXPLAINED

# 7.1 Evolution of New Engineering Materials

The development of engineering materials can broadly be understood through several technological stages.

The first stage involved the development and optimization of conventional materials such as steels, cast irons, aluminium alloys, copper alloys, ceramics, glass, polymers, and cement-based materials. The principal objective was generally to optimize mechanical performance, durability, manufacturability, and cost.

The second stage introduced advanced alloying, composite materials, fibre reinforcement, surface engineering, and controlled microstructures. Examples include precipitation-hardened alloys, nickel-based superalloys, carbon-fibre-reinforced polymers, ceramic-matrix composites, and high-performance polymers.

The third stage introduced nanotechnology and advanced characterization, enabling researchers to manipulate and measure material structures at increasingly small length scales. Graphene, carbon nanotubes, nanoceramics, nanocomposites, and two-dimensional materials emerged from this development.

The current stage is characterized by multiscale and multifunctional materials design. Composition, microstructure, nanoscale architecture, and manufacturing processes are increasingly optimized simultaneously.

High-entropy materials illustrate this transition particularly well. The original high-entropy alloy concept has expanded substantially, and high-entropy effects are now being investigated in metals, ceramics, polymers, composites, and low-dimensional materials (Hsu et al., 2024).

This evolution suggests that future materials development will increasingly depend on integration rather than isolated discoveries. A material may simultaneously be: compositionally complex; nanostructured; additively manufactured; architected; multifunctional; and  designed for recyclability This integrated approach represents a fundamental change in the philosophy of engineering materials. New engineering materials can be broadly classified into several overlapping groups as shown in Table 3.

Table 3: Classification of New Engineering Materials

| Material class | Representative examples | Principal characteristics | Major applications |
| --- | --- | --- | --- |
| High-entropy materials | HEAs, HE ceramics, high-entropy oxides, HE MAX/MXene | High compositional flexibility, strength, thermal/chemical stability | Aerospace, energy, nuclear, electronics |
| 2D materials | MXenes, graphene, transition-metal dichalcogenides | High surface area, electrical conductivity, tunable surfaces | Batteries, sensors, electronics, EMI shielding |
| Ultra-high-temperature materials | ZrB₂, HfB₂, TaC, HfC and composites | Extreme melting temperatures, oxidation/ablation resistance | Hypersonics, aerospace, nuclear |
| Metamaterials | Mechanical, acoustic, electromagnetic metamaterials | Properties controlled by architecture | Vibration control, impact protection, sensors |
| Aerogels | Silica, carbon, polymeric, bio-based aerogels | Ultralow density, high porosity, insulation | Thermal management, aerospace, filtration |
| Self-healing materials | Polymers, composites, concrete, coatings | Autonomous/intrinsic damage recovery | Infrastructure, aerospace, electronics |
| Nanocomposites | CNT/polymer, graphene/polymer, ceramic nanocomposites | Enhanced strength, conductivity, barrier properties | Structural, electronic and biomedical systems |
| Sustainable materials | Bio-based composites, CO₂-derived materials, recycled materials | Lower environmental impact, circularity | Construction, packaging, transport |
| Additively manufactured materials | AM alloys, ceramics, architected materials | Geometric and compositional freedom | Aerospace, biomedical, tooling |

Source: Wyatt, et al., 2024; Sun & Dai, 2024; Schweidler, 2024.

The boundaries between these classes are increasingly disappearing. For example, researchers are developing high-entropy MXenes, high-entropy ceramics, additively manufactured high-entropy alloys, and metamaterials incorporating nanocomposites.

# 7.2 High-Entropy Alloys and High-Entropy Materials

## 7.2.1 Development and fundamental concept

High-entropy alloys represent one of the most important developments in contemporary metallurgy. Unlike conventional alloys, which typically contain one dominant element, HEAs are composed of multiple principal elements in relatively substantial proportions. The high-entropy concept was initially developed primarily for metallic systems but has subsequently expanded into ceramics, oxides, carbides, borides, nitrides, polymers, composites, and other material classes. This broader family is now commonly described as high-entropy materials.

The scientific attraction of HEMs arises from their large compositional space. By varying the identity and concentration of multiple elements, researchers can potentially tailor several properties simultaneously. The resulting materials may exhibit complex local chemical environments, lattice distortions, compositional fluctuations, and metastable or multiphase structures. However, the traditional description of HEM behaviour in terms of four “core effects”, high configurational entropy, severe lattice distortion, sluggish diffusion, and cocktail effects, has increasingly been examined critically. Hsu et al. (2024) emphasize that these concepts should not be treated as universal explanations for all phenomena observed in high-entropy systems. This is an important point for future research because the high-entropy label alone does not guarantee superior performance. Actual properties depend on composition, processing, phase stability, microstructure, defects, interfaces, and service conditions.

    - Properties

HEAs can exhibit combinations of high strength; ductility; fracture toughness; wear resistance; corrosion resistance; thermal stability; magnetic behaviour; catalytic activity; and radiation tolerance. One important development has been the movement away from considering HEAs exclusively as structural materials. Recent work emphasizes their potential as multifunctional materials with electronic, electrochemical, magnetic, catalytic, hydrogen-related, and caloric functions (Han et al., 2024). This transition is important because engineering systems increasingly require materials that perform multiple functions simultaneously.

## 7.2.3 Processing and synthesis

## High-entropy materials can be produced through numerous routes, including: vacuum melting; arc melting; mechanical alloying; powder metallurgy; spark plasma sintering; physical vapour deposition; chemical synthesis; thermal spraying; and additive manufacturing. The synthesis method strongly affects phase constitution, grain size, segregation, porosity, residual stresses, and defect populations. Sun and Dai (2024) emphasize that controlled synthesis is a major issue because the compositional and structural complexity of HEMs makes it difficult to obtain precise control comparable to conventional materials.

## 7.3.1 High-entropy ceramics

High-entropy concepts have been particularly influential in ceramic research. High-entropy carbides, borides, oxides, nitrides, and other ceramics are being investigated for applications requiring combinations of hardness, thermal stability, corrosion resistance, electrical properties, and extreme-temperature performance. Recent literature continues to expand the field, with high-entropy ceramics being investigated for aerospace components, thermal protection systems, corrosion-resistant systems, and electromagnetic applications.

    - Applications

Potential applications of high-entropy materials include: aerospace structures; gas turbines; nuclear systems; energy storage; catalysts; hydrogen technologies; magnetic devices; wear-resistant coatings; biomedical materials; and thermal protection systems. Their application potential is particularly strong where multiple competing properties are required.

# 7.4 Two-Dimensional Materials and MXenes

## 7.4.1 Development

Two-dimensional materials are characterized by extremely small thicknesses, frequently approaching atomic or few-layer dimensions. Graphene stimulated extensive research in this area, but the field has subsequently expanded to transition-metal dichalcogenides, hexagonal boron nitride, phosphorene, MXenes, and other two-dimensional systems. MXenes are particularly important because they combine layered structures with electrically conductive transition-metal components and chemically active surfaces. Their surface chemistry can be modified through different terminal functional groups, which provides considerable opportunities for tailoring their interaction with ions, molecules, polymers, and biological systems.

    - Properties

## Important properties of MXenes include: high electrical conductivity; high specific surface area; hydrophilicity; mechanical flexibility; tunable surface chemistry; electrochemical activity; electromagnetic-wave attenuation; and ion transport capability.These properties make MXenes attractive for multifunctional engineering systems. Recent research has extended MXenes into three-dimensional architectures such as aerogels. A 2026 review, for example, identifies MXene-based aerogels as an emerging platform combining two-dimensional nanostructures with three-dimensional porous architectures.

    - Engineering applications

MXenes have been investigated for energy storage, their conductivity and surface chemistry makes them candidates for supercapacitors; lithium-ion batteries; sodium-ion batteries; zinc-ion batteries; and hybrid energy-storage systems. MXenes can be utilized as sensors. MXenes can interact with gases, ions, biomolecules, and mechanical deformation, enabling applications in chemical and physical sensing. Their conductivity makes them attractive for electromagnetic interference shielding in electronic and aerospace systems. They are used for electromagnetic shielding. The large surface area and tunable chemistry of MXenes facilitate research into adsorption, membrane separation, water treatment, and catalytic processes. They are applied in Environmental technologies. Potential applications include biosensors, drug delivery, tissue engineering, and other biomedical systems, although biocompatibility and long-term safety remain important research questions. They are also applied in Biomedical technologies.

  - Ultra-High-Temperature Ceramics

Ultra-high-temperature ceramics are among the most important material classes for extreme environments. They include transition-metal: carbides; borides; nitrides; and related composite systems. Materials such as hafnium carbide, tantalum carbide, zirconium diboride, and hafnium diboride have received considerable attention because of their extreme thermal stability. Wyatt et al. (2024) report that UHTCs can exhibit melting temperatures above 4,000 °C, high thermal conductivity, and very high stiffness. Their review also highlights developments involving additive manufacturing, high-entropy compositions, and two-dimensional materials as approaches for improving UHTC processing and performance.

    - Applications

The principal application areas include: hypersonic vehicles; spacecraft; atmospheric-entry vehicles; rocket nozzles; thermal protection systems; nuclear systems; high-temperature electronics. The need for such materials arises from increasingly severe engineering environments. Extreme environments can involve simultaneous high temperature, mechanical loading, oxidation, radiation, erosion, and thermal shock (Eswarappa Prameela et al., 2023).

    - Challenges

Despite their exceptional thermal properties, UHTCs have important limitations. The most significant include: intrinsic brittleness; limited fracture toughness; thermal-shock sensitivity; oxidation; processing difficulty; high sintering temperatures; machining difficulty; and high production costs. Research therefore increasingly focuses on composites, coatings, fibre reinforcement, additive manufacturing, and high-entropy UHTCs rather than relying exclusively on monolithic ceramics.

  - Metamaterials and Architected Materials

Metamaterials represent a major conceptual shift because their properties can be determined primarily by designed architecture rather than chemical composition. An architected material may be designed to exhibit: negative Poisson's ratio; programmable stiffness; controlled deformation; high energy absorption; vibration attenuation; unusual acoustic behaviour; optimized thermal transport. Additive manufacturing has been particularly important because complex lattice structures can be produced directly from digital designs. This development has important implications for lightweight engineering. Rather than making a conventional material thinner and accepting a corresponding reduction in stiffness, an engineer can design a cellular architecture that places material strategically where it contributes most effectively to load bearing.

    - Applications

Potential applications include: aircraft structures; automotive crash absorbers; vibration-control systems; protective structures; biomedical implants; robotics; and acoustic devices. The major challenge is that component-level performance depends strongly on manufacturing defects, surface roughness, fatigue, joints, and geometric imperfections. Consequently, research must increasingly move from idealized unit cells to realistic components and service conditions.

  - Aerogels and Advanced Porous Materials

# Aerogels are highly porous materials characterized by very low density and large internal surface area. Their properties arise from their three-dimensional porous network. Depending on composition, aerogels can provide: low thermal conductivity; low density; high surface area; acoustic insulation; adsorption capacity; and tunable electrical properties. Recent research has expanded aerogel development beyond conventional silica systems into carbon, polymeric, ceramic, cellulose, and hybrid aerogels. The combination of aerogels and MXenes is particularly promising because it can introduce electrical functionality into a lightweight porous structure. Recent literature describes MXene-based aerogels as an emerging multifunctional material platform.

    - Applications

Aerogels have potential applications in thermal insulation; aerospace; building materials; environmental remediation; filtration; energy storage; catalysis; sensors; biomedical systems. Their principal limitation is that excellent porosity and low density often occur at the expense of mechanical robustness. Research is therefore increasingly focused on reinforcement, hierarchical architectures, polymer integration, and advanced manufacturing.

  - Self-Healing Engineering Materials

Self-healing materials seek to address one of the fundamental limitations of conventional engineering materials: irreversible damage. The underlying concept is analogous, at a simplified engineering level, to biological healing. When damage occurs, a material should be capable of restoring part of its original function without complete replacement. Two principal approaches are commonly considered: Intrinsic self-healing, in which reversible molecular or physical interactions enable recovery, and extrinsic self-healing, in which healing agents are incorporated into the material. Potential applications include: polymer composites; coatings; concrete; flexible electronics; aerospace structures; and protective materials. The engineering significance of self-healing materials lies not only in repairing visible damage but potentially in preventing the progression of microdamage into larger defects. However, several challenges remain, including incomplete healing, limited healing cycles, dependence on environmental conditions, reduced properties after repeated healing, and difficulty validating long-term performance.

  - Advanced Nanocomposites

# Nanocomposites combine a conventional matrix with nanoscale reinforcement. Representative reinforcements include: graphene; carbon nanotubes; nanoclay; nanosilica; MXenes; ceramic nanoparticles; and metallic nanoparticles. Their potential arises from the exceptionally high surface area of nanoscale reinforcements and the importance of interfaces. A small quantity of nanomaterial can potentially influence: tensile strength; stiffness; fracture resistance; thermal conductivity; electrical conductivity; barrier performance; wear; and flame resistance. However, nanocomposite performance depends strongly on dispersion and interfacial bonding. Agglomeration can produce stress concentrations and negate the anticipated improvements. Consequently, future research needs to focus on controlled dispersion, scalable processing, interface engineering, and end-of-life recycling.

# Superwood

Superwood, this is the name of a new engineering material created by an American company called InventWood. If it’s called superwood, it must be so special. According to its creators, it’s 10 times stronger than steel and 6 times lighter (Sandra, 2025). Hu and his team have redesigned the inner structure of wood to make it more resistant without losing its lightness or its natural origin. The key behind the superwood’s success is the plants’ fibers that form the wood. Professor Liangbing Hu discovered how to strengthen the cellulose, which is the main element of plants’ fibers and, according to him ‘’the most abundant biopolymer on the planet.’’ To make this superwood possible, Hu removed a substance called lignin, which is the one that provides color and part of its strength. Then he focused on strengthening the cellulose, making the structure much denser and tougher. This process changed the appearance of the wood and transformed its resistance. This new wood was made by boiling in water and special chemicals to remove unwanted parts, like lignin, were added. It was then hot-pressed under extreme pressure, which makes the wood’s internal cells collapse and become compact. This compression increases its density, strength, and durability while keeping it lightweight. The entire process lasts about a week, and the final result is a wood with more resistance and lightness than many metals. After 3 years of its discovery, Hu got to improve the method and transform the superwood into a material ready to be sold.

Advantages in buildings and constructions made with superwood could be up to 4 times lighter than current ones, which would be a great advantage for engineering and safety. Constructions would be more resistant to earthquakes, easier to move, and faster to build. What’s more, since the superwood is still a natural material, it could help create more sustainable buildings (Sandra, 2025).

# 7.10 Sustainable and Bio-Derived Engineering Materials

The environmental impact of materials production has become increasingly important in engineering design. The conventional material-development model emphasizes:

performance → cost → manufacture → use → disposal.

A more sustainable approach considers:

performance → cost → resource use → manufacturing energy → emissions → durability → reuse → recycling.

Bio-derived materials based on cellulose, lignin, agricultural residues, natural fibres, and other renewable resources provide one route toward this objective. However, sustainability claims must be assessed carefully. A bio-based material is not necessarily environmentally superior if its production requires excessive water, energy, land, chemicals, or transportation.

Consequently, future material research should incorporate life-cycle assessment (LCA) from the early stages of development.

  - Additive Manufacturing as an Enabling Technology

Additive manufacturing is increasingly intertwined with the development of new engineering materials. Its advantages include: complex geometric freedom; material efficiency; customization; lattice fabrication; topology optimization; functionally graded structures; reduced tooling requirements. Its importance is particularly evident in high-entropy alloys and metamaterials. For high-entropy materials, additive manufacturing can influence solidification rate, grain structure, phase formation, segregation, and defect populations. For metamaterials, it allows complex lattice architectures that would otherwise be extremely difficult to manufacture. However, additive manufacturing itself introduces challenges such as: porosity; residual stress; cracking; surface roughness; anisotropy; process variability; limited production rate. Thus, additive manufacturing should not simply be viewed as a manufacturing solution; it is itself a complex materials-processing environment that changes the final material's microstructure and properties.

# 7.12 Artificial Intelligence and Data-Driven Materials Discovery

One of the most significant emerging trends is the application of artificial intelligence and machine learning to materials science. Traditional materials development is usually iterative:

Design → Synthesis → Characterization → Testing → Modification

This process can be expensive and time-consuming, particularly when the possible compositional space is enormous. AI and machine learning can potentially accelerate this process by identifying relationships between:

composition + processing + microstructure → properties.

This is particularly attractive for high-entropy materials because the number of possible compositions increases rapidly with the number of constituent elements. Future AI-enabled materials development may combine: computational thermodynamics; density functional theory; machine learning; molecular dynamics; high-throughput experimentation; automated synthesis; and automated characterization. The major challenge, however, is data quality. Machine-learning models are only as reliable as the datasets used to train them. Variations in testing methods, sample preparation, processing histories, and reporting standards can make materials databases difficult to combine.

# 7.13 Cross-Cutting Challenges

Despite their differences, new engineering materials face several common challenges. Laboratory synthesis often occurs in milligram, gram, or small-component quantities. Industrial applications may require tonnes of material or thousands of identical components. Scaling up is a major challenge.

The transition between these scales is frequently non-trivial. Advanced precursors, specialized equipment, energy-intensive processing, and complex quality-control procedures can make emerging materials expensive. Reproducibility is another major challenge. Complex materials can be highly sensitive to: composition; processing temperature; cooling rate; atmosphere; impurities; grain size; and defects. Small variations can therefore produce significant property differences. Many emerging materials have not yet been subjected to decades of service-equivalent testing. Long-term studies are required for: fatigue; creep; oxidation; corrosion; radiation damage; thermal cycling; environmental degradation. Reliability is an issue. The environmental footprint of advanced materials should include raw-material extraction, processing, transportation, use, and end-of-life treatment. This will reduce environmental impact. Industrial adoption requires reliable standards for: characterization; quality control; failure analysis; lifetime prediction; environmental performance; and recycling. Standardization currently is an issue (Eswarappa, et al., 2023; Han, et al., 2024; Hsu, et al., 2024; Scheweidler, et al., 2024; Sun & Dai, 2024).

8. NEW ENGINEERING MATERIALS AND THE BUILD-UP TO A SELF-RELIANT ECONOMY

New engineering materials development in Nigeria will lead to self-reliance this is because new materials development is value addition, a product of further processing of ores and raw resources. It is an established fact that value addition adds value to new materials, increasing their benefits over raw materials and ores when sold in their virgin form. New materials creates new jobs and new technologies. They bring about development, reduce imports, and promote export, and encourage entrepreneurship this then leads to economic and industrial development which results in self-reliance and self-sufficiency.  New engineering materials development value chain is a sine quo non in the build-up to a self-reliant Nigeria (Ihom & Odeh, 2025).

## 8.1 Strategies for Building a Self-Reliant Nigerian Economy

### Promote Agricultural Modernization

Nigeria should increase agricultural productivity through: improved seeds and agricultural inputs; irrigation; mechanization; extension services; agricultural research; rural roads; storage facilities; cold-chain infrastructure; agricultural insurance; and access to affordable finance. Agricultural policy should also encourage the integration of farming with agro-processing and manufacturing.

### 8.1.2 Develop Agro-Processing Industries

Agricultural production should be connected to domestic processing industries. For example:

Cocoa → cocoa processing → chocolate and related products

Cassava → starch, flour, ethanol and other industrial products

Cotton → textile production → garments

Oil palm → edible oils, oleochemicals and other products

Such value chains can generate employment while increasing domestic value capture.

### 8.1.3 Strengthen Manufacturing

Nigeria should develop competitive manufacturing capabilities in areas where domestic production has strong economic potential. Priority areas can include food processing, pharmaceuticals, textiles, construction materials, machinery, chemicals, petrochemicals, automotive components, renewable-energy equipment, and other intermediate goods. Industrial policy should focus on productivity and competitiveness rather than indefinite protection from competition. New engineering materials development will contribute seriously in strengthening the manufacturing sector.

### 8.1.4 Invest in Reliable Energy

Improving electricity generation, transmission, and distribution should remain a major development priority. Nigeria can also diversify its energy system through solar, hydro, gas, wind where commercially appropriate, and other technologies. Energy policy should emphasize reliability, affordability, investment, and sustainability. New engineering materials development will provide the materials to be utilized in developing the energy sector as explained above.

### 8.1.5 Strengthen Technical and Vocational Education

Polytechnics, technical colleges, vocational centers, universities, and private-sector employers should work together to develop skills relevant to manufacturing, construction, agriculture, engineering, ICT, energy, and other sectors. Industry-based apprenticeships and practical training can complement conventional academic education. Strengthening technical and vocational education will provide the necessary manpower for new engineering materials development.

### 8.1.6  Promote Research, Development, and Innovation

Nigeria should strengthen funding and institutional support for research and development. Universities and research institutions should establish stronger partnerships with industries so that research findings can be converted into commercially viable technologies, products, and processes. Promotion of research, development and innovation will lead to new engineering materials development and self-reliance.

### Develop Domestic Financial Markets

Greater economic self-reliance requires stronger domestic financial institutions. Policies can encourage: long-term industrial lending; venture capital; development finance; pension-fund investment in productive assets within appropriate regulatory frameworks; agricultural finance; SME financing; and domestic capital-market development.

### 8.1.8 Improve the Business Environment

Government can support domestic production by simplifying regulations, improving tax administration, reducing unnecessary bureaucratic barriers, strengthening contract enforcement, and improving regulatory coordination.

### 8.1.9 Encourage Local Supply Chains

Government procurement and industrial policies can, where economically justified and consistent with applicable trade obligations, encourage domestic suppliers to participate in public and private supply chains. However, local-content policies should be accompanied by measurable productivity and quality standards.

### Promote Export Diversification

Nigeria should progressively expand exports beyond crude petroleum. Potential areas include: processed agricultural products; manufactured goods; petrochemicals; solid minerals after appropriate processing; digital services; creative industries; professional services; and selected renewable-energy and technology products. Diversification of export of new engineering materials will promote self-reliance.

### 8.1.11 Strengthen Regional Trade

Nigeria's large domestic market provides a significant foundation for industrialization, while regional markets can provide additional opportunities. Participation in the African Continental Free Trade Area can provide opportunities for Nigerian firms to expand into African markets, provided domestic businesses are sufficiently productive and competitive.

### 8.1.12 Maintain Strategic but Open International Trade

Self-reliance should not result in indiscriminate restrictions on imports. Imports of machinery, industrial inputs, medical technologies, scientific equipment, and other productivity-enhancing goods can support domestic production. Trade policy should therefore distinguish between imports that undermine productive capacity and imports that strengthen it.

### 8.1.13 Improve Public Institutions and Accountability

Long-term self-reliance requires effective institutions. Government should strengthen transparency, accountability, public financial management, procurement systems, regulatory institutions, and the rule of law (WTO, 2023).

9. CHANGING THE STATUS QUO.

## Changing the status quo of Nigeria’s current status as an economic dependent country which imports most of what she needs and export most of her resources in crude or raw form only to turn and import all her refined products, will only change when the country starts doing the right thing by implementing the above stated measures for a self-reliant economy. The absence of value addition in Nigeria will only prolong her status as an economically dependent country living at the mercy of economically self-reliant countries. Below is a proposed Framework for Nigeria’s economic self-reliance:

## A Proposed Framework for Nigeria's Economic Self-Reliance

A useful framework can be represented as follows:

Domestic Resources

↓

Infrastructure + Energy + Finance

↓

Human Capital + Technology + Entrepreneurship

↓

Agricultural and Industrial Production

↓

Value Addition and Local Supply Chains

↓

Competitive Domestic Markets

↓

Diversified Exports

↓

Employment + Income + Foreign Exchange

↓

Economic Resilience and Sustainable Development

## Figure 1: A Proposed Framework for Nigeria's Economic Self-Reliance

This framework demonstrates that self-reliance is not achieved through a single policy. It is the result of interactions among infrastructure, skills, technology, finance, institutions, production, markets, and international trade. ,” this provides a strong basis for arguing that Nigeria's next stage of development should focus on converting its macroeconomic stabilization into productive capacity, local value addition, industrialization, technological development, agricultural transformation, and inclusive employment. New engineering materials development is normally driven by the need for higher performing materials and they dictate new technologies and better performing products and machineries being a product of value addition they contribute to self-reliance and if developed in Nigeria, definitely Nigeria will move from a dependent country to a self-reliant and self-sufficient country (Rodrik, 2004; UNCTAD, 2020; WTO, 2023; CBN, 2023; WB, 2024; ADB, 2024).

10. CONCLUSION

The review “New Engineering Materials Development for a Self-Reliant Nigerian Economy’’ has been critically examined and the following conclusions drawn:

1. Conventional materials have been taken to their limits by current and advanced technology. Conventional engineering materials such as steels, aluminium alloys, titanium alloys, ceramics, polymers, concrete, and fibre-reinforced composites have enabled major developments in transportation, infrastructure, manufacturing, energy generation, and aerospace technology. Nevertheless, the increasing complexity of modern engineering systems has exposed important limitations in the performance envelope of conventional materials.

2. The study covers engineering materials developed from 2020 to 2026 and the new trend of engineering materials development.

3. New engineering materials development for a self-reliant economy is synonymous with value addition. Value addition is one of the characteristics of a self-reliant economy.

4. Nigeria is typically a country with an import dependent economy the paper has fully emphasized the need for value addition for the country to be self-reliant.

5. The country is an import-dependent country with an economy that is dependent; selling crude and raw resources while importing refined products at higher prices.

6. The absence of value addition in Nigeria will only prolong her status as an economically dependent country living at the mercy of economically self-reliant countries

7. The current stage in new engineering materials development is characterized by multiscale and multifunctional materials design. Composition, microstructure, nanoscale architecture, and manufacturing processes are increasingly optimized simultaneously

8. High-entropy materials illustrate this transition particularly well. The original high-entropy alloy concept has expanded substantially, and high-entropy effects are now being investigated in metals, ceramics, polymers, composites, and low-dimensional materials.

9. This evolution suggests that future materials development will increasingly depend on integration rather than isolated discoveries. A material may simultaneously be: compositionally complex; nanostructured; additively manufactured; architected; multifunctional; and  designed for recyclability This integrated approach represents a fundamental change in the philosophy of engineering materials.

REFERENCES

African Development Bank. (2024). African economic outlook 2024: Driving Africa's transformation: The reform of the global financial architecture. African Development Bank.

Central Bank of Nigeria. (2023). Annual report and financial statements for the year ended 31 December 2023. Central Bank of Nigeria.

Eswarappa, P, S., Pollock, T. M., Raabe, D., Meyers, M. A., Aitkaliyeva, A., Chintersingh, K.-L., Cordero, Z. C., Graham-Brady, L., & others. (2023). Materials for extreme environments. Nature Reviews Materials, 8, 81–88. https://doi.org/10.1038/s41578-022-00496-z

Han, L., Zhu, S., Rao, Z., Scheu, C., Ponge, D., Ludwig, A., Zhang, H., Gutfleisch, O., Hahn, H., Li, Z., & Raabe, D. (2024). Multifunctional high-entropy materials. Nature Reviews Materials, 9, 846–865. https://doi.org/10.1038/s41578-024-00720-y

Hsu, W.-L., Tsai, C.-W., Yeh, A.-C., & Yeh, J.-W. (2024). Clarifying the four core effects of high-entropy materials. Nature Reviews Chemistry, 8, 471–485. https://doi.org/10.1038/s41570-024-00602-5

Ihom, A.P. and Offiong, A. (2018) Intelligent and Smart Materials Pioneering, a New Technological Era in the 21st Century: A Review Paper, JORIE, 3(1), 1-14.

Ihom, A.P., Odeh, E.U., Onche, E.O., Aondona, P.T., Bassey, J.M., and Emenike, U.O.W.

(2023): Investigating the Effects of SiC Particles Addition and Thermal Treatment on 90%Al-

10% Cu alloy, IJFETR, 2023, 04(02), 016-032. Article DOI: https://doi.org/10.53294/ijfetr.2023.4.2.0015

Ihom, A.P. and Odeh, E. U. (2025) Exploration, Exploitation, and Value Addition of Energy Materials for Sustainable Energy Usage and Economic Development in Africa: A Review; DOI: 10.56201/ijemt.vol.11.no10.2025.pg171.196.

IMF (2026) Report on the performance of the Nigerian Economy

Jain, R.K. (2009) Production Technology, 16TH Edition, India: Khanna Publishers.

Ogbodo J.N, Ihom, A.P., Offiong, A., Moses, S.A. and Denis, U.I. (2015) Corrosion Resistance Characterisation of 90Al-10Cu/ 4SiC Metal-Matrix  Particulate Composite (MMPC) in Some Selected Media, Journal of Multidisciplinary Engineering Science and Technology (JMEST) ISSN:3159-0040 Vol. 2 Issue 8, August – 2015,

Organisation for Economic Co-operation and Development. (2023). OECD economic surveys: Nigeria 2022. OECD Publishing. https://doi.org/10.1787/33c5c06f-en

National Bureau of Statistics. (2023). Nigeria GDP report. National Bureau of Statistics.

Reuters (2026) Report on Nigerian Economy in 2026.

Rodrik, D. (2004). Industrial policy for the twenty-first century. CEPR Discussion Paper No. 4767. Centre for Economic Policy Research.

Sandra, V. (2025) Goodbye to Steel-the ‘’Superwood’’ Created by InventWood, Promises lighter, Safer, and More Sustainable Buildings, Publication of UniÓn Rayo EN.

Schweidler, S., Botros, M., Strauss, F., Wang, Q., Ma, Y., Velasco, L., Marques, G. C., Sarkar, A., Kübel, C., Hahn, H., Aghassi-Hagmann, J., Brezesinski, T., & Breitung, B. (2024). High-entropy materials for energy and electronic applications. Nature Reviews Materials, 9, 266–281. https://doi.org/10.1038/s41578-024-00654-5

Sun, Y., & Dai, S. (2024). Synthesis of high-entropy materials. Nature Synthesis, 3, 1457–1470. https://doi.org/10.1038/s44160-024-00690-7

United Nations Conference on Trade and Development. (2020). Impact of the COVID-19 pandemic on trade and development: Transitioning to a new normal. United Nations.

Wyatt, B. C., Nemani, S. K., Hilmas, G. E., Opila, E. J., & Anasori, B. (2024). Ultra-high temperature ceramics for extreme environments. Nature Reviews Materials, 9, 773–789. https://doi.org/10.1038/s41578-023-00619-0

World Bank. (2022). Nigeria development update: The continuing urgency of business unusual. World Bank.

World Bank. (2024). Nigeria development update: Staying the course on reforms. World Bank.

World Trade Organization. (2023). Trade policy review: Nigeria. World Trade Organization.