SHIELDING GASES FOR STAINLESS STEELS &

CORROSION RESISTANT ALLOYS

| ALLOY GRADES | PULSE or GMAW | GTAW | PURGING GAS |
| --- | --- | --- | --- |
| 301, 302, 303, 304L, 316L, 321 Austenitic | 2.0mm – 10mm 2% CO2 Bal Argon 2% O2 Bal Argon OR 12mm > 20 – 25% He 2% + CO2 Bal ARGON | ARGON | ARGON or 100% NITROGEN |
| 310, 253MA Austenitic | 25% He Bal ARGON OR 100% ARGON | ARGON | ARGON or 100% NITROGEN |
| SAF 2205, SAF 2304 Duplex | 20% - 25% He + 2% CO2 Bal ARGON 2% O2 Bal ARGON OR 2% CO2 Bal ARGON | ARGON OR 2% N2 Bal ARGON | 2% N2 Bal ARGON OR 100% N2 |
| SAF 2507 Super duplex | 3.0mm – 8.0mm 2% O2 Bal ARGON Or 2% CO2 Bal ARGON 10 mm > 20 – 25% He + 2% CO2 Bal ARGON OR ARGON | 2% N2 Bal ARGON | 2% N2 Bal ARGON OR 100% NITROGEN |
| 430, CR12 HT, 5CR12 Ti 3CR12 Ferritic | 3.0mm – 8.0 mm 2% CO2 Bal ARGON 2% O2 Bal ARGON 10mm > 20% - 25% He 2% + CO2 Bal ARGON | ARGON | ARGON OR 100% N2 |
| Sanicro 31HT, Sanicro 70, Sanicro 72, Ultimet, Hastelloy C-22 & C-276 (Nickel alloys) | 20% - 25% He 2% + CO2 Bal ARGON 25% He Bal ARGON ARGON | ARGON | ARGON OR ARGON + He |
| *Note*The above grades of material can be both [Pulse and standard MIG] welded with the above gas percentages |  |  |  |

Note: Gas suppliers are omitted on this chart, gas percenatges listed should serve as a guide only, an extra 1. 0 % < > is permissable